| GREY PORTLAND CEMENT OPS 42.5 N |
| --- |
| Mark | grey portland cement OPC 42.5 N |
| Standard | British Standards 12/1996 or ASTM C-150 |
| Origin | Ukraine |
| Delivery | FOB Ports of the Black and Azov seas |
| Packing | Big-Bag or 50 Kg Bags |
| Inspection | SGS at Seller’s cost |
| CEMENT - 42.5 N : Chemical Composition |  |
| SILICON DIOXIDE (SIO2) | 21.00 |
| ALUMINIUM OXIDE (AL2O3) | 5.30 |
| FERRIC OXIDE (FE2O3) | 3.30 |
| CALCIUM OXIDE (CAO) | 65.60 |
| MAGNESIUM OXIDE (MGO) | 1.10 |
| SULPHUR TRIOXIDE (SO3) | 2.70 |
| LOSS OF IGNITION (LOI) | 0.90 |
| TRICALCIUM SILICATE (C3S) | 60.00 |
| DICALCIUM SILICATE (C2S) | 15.00 |
| TRICALCIUM ALUMINATE (C3A) | 8.05 |
| TRICALCIUM ALUMINO FERRICE (C4AF) | 9.76 |
| CEMENT - 42.5 N : Physical and Mechanical Properties |  |
| BLAIN CM2/GR | 3.250 |
| AUTOCLAVE EXPANTION | 0.02 |
| INITIAL SETTING TIME (VICAT) | 105 MINUTES |
| FINAL SETTING TIME (VICAT) | 135 MINUTES |
| COMPRESSIVE STRENGTH | @ 03 DAY'S 230 KG/CM2 |
|  | @ 07 DAY'S 305 KG/CM2 |
|  | @ 28 DAY'S 420 KG/CM2 |